## Slide 1
Plasmonic nanomaterials for
ultrafast nonlinear optics and photochemistry
Anatoly V Zayats
www.nano-optics.org.uk

## Slide 2: Plasmonic nanomaterials
Active and nonlinear hyperbolic &
hybrid dielectric metamaterials
Metasurface
holography
Plasmonic hot-electrons for
photochemistry & catalysis
Bio- & gas
sensing
New plasmonic
materials
Topological photonics
Ultrafast and nonlinear
nanophotonics
Controlling
chirality
OAM and metamaterials

## Slide 3
Nonlinear materials
J. Phys.: Photon. 6, 032502 (2024).

## Slide 4
Nonlinear materials
J. Phys.: Photon. 6, 032502 (2024).

## Slide 5: Plasmonic hot electrons
control
Dem(Te) = DReem+ DImem
Laser Phot. Rev. 12, 1700082 (2018); eLight 4, 15 (2024).
Metal (gold)
Optical nonlinearity of an electron gas: due to hot electrons

## Slide 6: Hot electrons in metals
~10 fs
~500 fs
~5 ps
time
e-
h+
0 s
e-
e-e scattering
e-ph scattering
e-
Material platform choice
Nanostructure geometry
eLight 4, 15 (2024).

## Slide 7: Hot electrons in metals
~10 fs
~500 fs
~5 ps
time
e-
h+
0 s
e-
e-e scattering
e-ph scattering
e-
Material platform choice
Nanostructure geometry
Nonlocal response
Quantum effects
eLight 4, 15 (2024).

## Slide 8
Plasmonic hot electrons
Nonlinear optics: Photochemistry:
hot-electron transfer
Short-lived electrons: Long-lived electrons
(fast electron relaxation) (slow electron relaxation)
Material platform choice
Nanostructure geometry
Dem(Te) = DReem+ DImem

## Slide 9
Plasmonic metaparticles

## Slide 10
Nanoscale Adv. 3, 767 (2021); Faraday Discussions 214, 385 (2019).
Plasmonic heterostructures
SiO2: support-
large surface
area
Au: LSP excitation-
hot-electron generation
Pt: molecular adsorption & hot hot-electron extract

## Slide 11
Nanoscale Adv. 3, 767 (2021); Faraday Discussions 214, 385 (2019).
Plasmonic heterostructures
Optical properties and hot electron generation

## Slide 12
Nanoscale Adv. 3, 767 (2021); Faraday Discussions 214, 385 (2019).
Plasmonic heterostructures
Hot-electron induced degradation of methylene blue on Au/Pt nanostructure

## Slide 13
Hot-electron dynamics
probe
pump
Nanophotonics 10, 2929 (2021).

## Slide 14
Au: 10-15 nm; Pt: 1-2 nm
Hot-carrier dynamics in Au/Pt heterostructures: in water.
Hot-electron dynamics
Nanophotonics 10, 2929 (2021).

## Slide 15
Hot-electron dynamics
Nanophotonics 10, 2929 (2021).
Hot-carrier dynamics in Au/Pt heterostructures: in water and glycerol.
Au: 10-15 nm; Pt: 1-2 nm

## Slide 16
Ultrathin monocrystalline plasmonic nanofilms

## Slide 17
Nature Comm. 15, 2840 (2024).
Monocrystalline ultrathin gold

## Slide 18
Nature Comm. 15, 2840 (2024).
Monocrystalline ultrathin gold
Atom layer etching

## Slide 19
Towards goldphene
Nature Comm. 15, 2840 (2024).
Ultrathin monocrystalline gold (and other plasmonic metals)
(transdimensional materials family: Boltasseva & Shalaev)

## Slide 20
Towards goldphene
Nature Comm. 15, 2840 (2024).
Ultrathin monocrystalline gold (and other plasmonic metals)
Ag
Cu

## Slide 21
Nature Comm. 15, 2840 (2024).
SHG & THG
Towards goldphene

## Slide 22
Nature Comm. 15, 2840 (2024).
SHG & THG
Towards goldphene
IEEE J. Quant. Electr.
31, 2044 (1995):
Nb ultrathin films

## Slide 23
Nature Comm. 15, 2840 (2024).
SHG & THG quantum confinement effects
bulk
20 layers
10 layers
Towards goldphene

## Slide 24
Nature Comm. 15, 2840 (2024).
SHG & THG quantum confinement effects
bulk
20 layers
10 layers
Towards goldphene
quantum effects:
anisotropic gold

## Slide 25
Nature Comm. 15, 2840 (2024).
SHG & THG quantum confinement effects TPPL
bulk
20 layers
10 layers
Towards goldphene

## Slide 26
Nature Comm. 15, 2840 (2024).
Monocrystalline ultrathin gold
Nature Comm. 15, 703 (2024).

## Slide 27
Nature Comm. 15, 703 (2024).
Ultrathin and ultrafast
Sub-picosecond dynamics: Au/SiO2

## Slide 28
Ultrathin and ultrafast
Nature Comm. 15, 703 (2024).
Nonthermalised electron scattering rate: MC – 18 THz, PC – 24THz.

## Slide 29
Nature Comm. 15, 703 (2024).
Hot-carrier cooling at a metal-semiconductor interface:
- nearly theoretical transfer rate despite a smooth interface (~ 10%)
- electron-phonon thermalisation time increases: thin-film effects
- substrate phonon effects for MC ultrathin films
Ultrathin and ultrafast

## Slide 30
Monocrystalline CuS

## Slide 31
Mesoscopic CuS
ACS Nano 13, 6550 (2019).
covellite (CuS) nanoscrystals: monolayer of
thickness 4-10 nm nanocrystals
size: 15-200 nm
p-type “metal”
free-carrier concentration: ~ 3x1021 cm-3
c.f. Au, Ag: ~ 6x1022 cm-3

## Slide 32
Mesoscopic CuS
ACS Nano 13, 6550 (2019).
anisotropic dielectric
hyperbolic material: ENZ properties
anisotropic plasmonic material

## Slide 33
Mesoscopic CuS
Nonthermalised carrier dynamics
Laser Phot. Rev. 15, 2000346 (2021).

## Slide 34
Mesoscopic CuS
Laser Phot. Rev. 15, 2000346 (2021).
Nonthermalised carrier dynamics:
nonlocal effects

## Slide 35
Electron dynamics in ultrathin monocrystalline plasmonic nanofilms
Time-varying quadratic nonlinearity of ITO

## Slide 36
Enhancing natural ENZ nonlinearity
Nano Lett. 20, 5421 (2020).
Plasmonic-ENZ metasurface:
~ 104 SHG enhancement (exp)

## Slide 37
Nano Lett. 24, 3744 (2024).
Time-dependent quadratic nonlinearity

## Slide 38
Nano Lett. 24, 3744 (2024).
Linear changes:
SHG changes:
Time-varying SHG >> time-varying linear T
Time-dependent quadratic nonlinearity

## Slide 39
Nano Lett. 24, 3744 (2024).
Renormalisation of the plasma frequency:
~ 40 nm
Time-varying second-order nonlinear susceptibility: ~ 10%
Time-dependent quadratic nonlinearity

## Slide 40
Nano Lett. 24, 3744 (2024).
Renormalisation of the plasma frequency:
~ 40 nm
Time-varying second-order nonlinear susceptibility: ~ 10%
Time-dependent quadratic nonlinearity
Miller’s rule for nonlinear susceptibility:
Nonlinear dipole density:

## Slide 41
Nano Lett. 24, 3744 (2024).
Renormalisation of the plasma frequency:
~ 40 nm
Time-varying second-order nonlinear susceptibility: ~ 10%
Coupling to resonant plasmonic metasurface:
- 10-fold enhancement
- control of circular polarised SHG
Time-dependent quadratic nonlinearity

## Slide 42
Ultrafast nonlinear plasmonics
J. Phys.: Photon. 6, 032502 (2024).
Time (ps)
-1
1
25
Wavelength (nm)
480
750

## Slide 43
Unidirectional chiral scattering

## Slide 44
Nature Comm. 16, 1125 (2025).
Unidirectional emission by rotating chiral dipoles

## Slide 45
Nature Comm. 16, 1125 (2025).
Unidirectional emission by rotating chiral dipoles

## Slide 46
Nature Comm. 16, 1125 (2025).
620 nm
950 nm
860 nm
Unidirectional emission by rotating chiral dipoles

## Slide 47
@KingsNanoOptics

## Slide 48
nano-optics.org.uk
@KingsNanoOptics